5423 U. H. M. W. Polyethylene Tape

Product Data Sheet

Updated 	:   March 1996

Supersedes	:	  October 1993

Product Description

|  | A low friction clear abrasion resistant tape which is resistant to puncturing, gouging etc., coated with an aggressive rubber resin adhesive. |
| --- | --- |

Physical Properties

Not for specification purposes

Adhesive Type

|  | Rubber resin. |  |
| --- | --- | --- |

Backing

|  | Ultra-high molecular weight polyethylene |
| --- | --- |
| Tape Thickness (ASTM D-3652) |

280 µm

Release Liner

|  | Silicone Treated paper |
| --- | --- |

Tape Colour

|  | Cream |
| --- | --- |
| Shelf Life | 12 months from date of despatch by 3M when stored in the original carton at 21°C (70°F) & 50 % Relative Humidity |

Performance Characteristics

Not for specification purposes

Adhesion to Stainless Steel ASTM D-3330

2.8 N/10mm

Tensile Strength

ASTM D-3759

96.3 N/10mm

Elongation at Break

ASTM D-3759

|  | 500.00 % |
| --- | --- |

Temperature Range

Maximum

Minimum

105 °C

-35 °C

Date :	  March 1996

5423 U. H. M. W. 		Polyethylene Tape

Additional Product Information

|  | UHMW POLYETHYLENE is a thermoplastic that has unique combination of properties which makes it ideal for tough impact wear or sliding applications. | No. 5423 is a thick clear UHMW Polyethylene tape developed to extend service life as a protective surface against extreme wear. | The liner on 5423 makes it possible to fabricate or die-cut the backing into various lengths and shapes. |
| --- | --- | --- | --- |

|  | Application Techniques | Best results are attained when applied to a clean, dry and non dusty surface above 0°C. | To improve adhesion ensure firm and even application pressure is applied. |
| --- | --- | --- | --- |

Applications

Conveyor flat guide rails.

Discharge chutes.

Spiral wrap for round guide rails.

Glue sealing plates.

Rotor blades.

Spray booth liners.

Tank and bin liners.

Drawer and cabinet slides.

Feed and grain chutes.

Packing table tops.

Date :	  March 1996

5423 U. H. M. W. 		Polyethylene Tape

| FEATURES | ADVANTAGES | BENEFITS |
| --- | --- | --- |

Tough UHMW Polyethylene.

High tack rubber resin adhesive.

Resists abrasion and wear under load.

Resists high impacts.

Puncture and gouge resistant .

High energy absorption.

Release surface for sticky resinous or viscous materials.

Inert to most chemicals and solvents.

Reduces friction which promotes movement.

Prevents marking or scratching

of product.

Adheres instantly to most surfaces.

Good long ageing bond strength.

Saves money by reducing repairs or replacement of parts or equipment.

Reduces noise and lessens worker fatigue.

Reduces clean up and maintenance costs.

Protects surfaces prolonging life of parts or equipment.

Increases production speeds and reduces rejects, increases equipment efficiency.

Easy to apply.

Remains in place under stress prolonging life of equipment.

3M is a trademark of the 3M Company.